H11	CURTAIN WALLING

To be read with Preliminaries/General conditions.

TYPE OF CURTAIN WALLING

H11/110	CURTAIN WALLING REF:

-	Drawing reference(s):

- Supporting structure: As detailed on drawings. Structural horizontal supports for curtain walling generally at ….mm from FFL and ….mm from FFL.

- Curtain walling system:

Manufacturer and reference: 	COMAR ARCHITECTURAL ALUMINIUM SYSTEMS

Unit 5, The Willow Centre,

17, Willow Lane,

Mitcham,

Surrey CR4 4NX

Telephone: 020 8685 9685

Fax:           020 8646 5096

e-mail: Sales@Parksidegrp.co.uk

Type: COMAR 6 mullion drained, ladder frame system, stick build, step or square cut, pressure equalised and drained in accordance with BS6262. External pressure plates, seals and cappings fixed on internal mullions and transoms. To include all products, fixings and interfaces necessary to complete fabrication and installation. Performance criteria to comply with Design/Performance Requirements and Testing subsections.

Comar 6EFT Curtain Wall Systems
An insulated curtain wall system, suitable for all heights, including glazed roofing applications for new and refurbished projects. Comar 6EFT Curtain Walling System is available in ladder frame and stick build configurations.
Comar 6EFT is available with the following options:
Comar 6EFT Curtain Wall:
Eenables the construction of sheer high-rise as well as sloped and inclined facades. Thermally efficient with standardised 50mm profiles, custom-made profiles are available on request.
Comar 6EFT 4sided SG:
Creates a façade with no visible aluminium sight lines. Thermally efficient, the external sight-line is created with a 20mm EPDM joint seal. This joint can also be made from silicon sealant.
Comar 6EFT 2sided SG:
Enables vertical or horizontal sightlines. A bespoke finish can be achieved through using a variety of cover caps.
Thermally efficient dependent upon the selection of vertical or horizontal lines the structurally glazed side is achieved with a 20mm EPDM joint seal. This joint can also be made with silicon sealant.
Both vertical and horizontal options use standard 50mm profiles.
Comar 6 EFT Facetted:
Allows the creation of external and internal curves as well as 90° corners.
Facets or segments can be created from 0° with the unique option to create the curve internally or externally.
Comar 6EFT Curtain Walling System offers the following features:
Material: 
The system is constructed from extruded aluminium profiles, using aluminium alloy: 6063 complying with the requirements of BS 1474.
The thermal barrier system is achieved by means of PVC/PP extrusions.
Finishes:
Available in RAL, Syntha-Pulvin and BS colours.
Aluminium profiles are finished to the following specifications:
Silver/Bronze/Black anodising AA25 to BS EN 12373-1: 2001 or BS 3987.
Liquid organic coating to BS 4842: 1984.
Polyester powder coating to BS 6496:1984.
Weather Performance
Comar 6EFT achieved the following:
Air permeability:
Curtain Wall: Class AE 750 (to EN 12152)
EFT Vent: Class 4 (to EN 12207)
Water tightness:
Curtain Wall: Class RE 750 (to EN 12154)
EFT Vent: Class E 750 (to EN 12208)
Wind resistance:
Curtain Wall: 2400 Pa design, 3600 Pa safety (to EN 13116)
EFT Vent: 2400 Pa design, 3600 Pa safety (to EN 13116)
Drainage:
Comar 6EFT is a mullion drained system which meets the requirements of ‘ventilated and drained glazing system’ as specified in BS 6262.
Façade Cover Caps:
A variety of cover caps are available for this system. The slimmest sightlines can be achieved using a 50mm wide cap, which is double chamfered to provide a visible face of 16mm. Cover caps have a typical edge radius of 1.5mm for even distribution of the powder coating layer.
Windows
Comar 6EFT Concealed Vents:
Top or hung windows integrate directly into the curtain wall. Concealed vents have no exterior sight-line which means that when closed the façade maintains the same slim sightline.
Consult Comar Architectural Aluminium Systems technical literature for details. Comar Architectural Aluminium Systems can also provide a design and specification service and it is recommended that they are consulted early in the design process.

- Internal framing member:

Material: Aluminium extrusion from alloy 6063 T5or T6, with or with internal reinforcement as required. COMAR mullion. COMAR transom Square cut. Mullions to run continuous with intermediate horizontal transoms.

Seals to be COMAR EPDM GASKETS Internal gaskets to be glued frames to required size.

- Finish: Polyester powder coated to BS6496 by manufacturer (RAL) or anodised to BS  -----

- Colour/texture: to standard RAL colour (   ) .

- Minimum film thickness: Coverage to be not less than 40 microns. Gloss level   %

-	External cover cap:

Material: As internal framing member, but joints will be allowed at COMAR/Architects’ approved positions.

Finish: As internal framing member

Colour/texture: As internal framing member

Minimum film thickness: As internal framing member

- Glazing: Double glazed pre-sealed units manufactured to BS 5713.

Pane assembly

Inner pane:

Outer pane:

Outer pane:

Glazing system:

Glass setting block to be at 120mm from outside edge of transom.

-	Panel/facing type:

If panel has external/internal linings

External material: e.g.

External finish:

Internal material: ______

Internal finish: ______

Core insulation: ______

-	Accessories:

-	Incorporated components:

-	Other requirements:

H11/130	BRISE SOLEIL

-	Drawing reference(s):

- Manufacturer and reference: 	COMAR ARCHITECTURAL ALUMINIUM SYSTEMS

Unit 5, The Willow Centre,

17, Willow Lane,

Mitcham,

Surrey CR4 4NX

Telephone: 020 8685 9685

Fax:           020 8646 5096

e-mail: Sales@Parksidegrp.co.uk

-	Material: Aluminium as clause 710

-	Finish: Polyester powder coated

Colour/texture:

Minimum film thickness:

-	Fixing: From curtain wall or structure

-	Other requirements: